Electric Arc Furnace

Comments

Run Information

| User Id | taehee0518@daum.net |
| --- | --- |
| Date | 13/07/2024 10:07:33 |
| Status | 1 |
| Score | $ 460.09 |

Simulation settings

| User Level | University Student |
| --- | --- |
| Steel Grade | Engineering Steel |

Cost Breakdown

| Time (in minutes) | 75 |
| --- | --- |
| Tapping mass | 86 |
| Tap temperature | 1643 |
| Total Energy | 35370 kWh |
| Total Energy | 409 kWh/t |
| Power | $ 1946 |
| Scrap | $ 75 |
| Additions | $ 17080 |
| Other consumables | $ 20161.07 |
| Total Cost | $ 39755 |
| Cost Per Tonne | $ 460.09 |

Steel Composition / wt%

| Element | Current | Min | Max |
| --- | --- | --- | --- |
| C | 1.090 | 1.050 | 1.150 |
| Si | 0.106 | 0.100 | 0.150 |
| Mn | 0.223 | 0.150 | 0.250 |
| P | 0.007 | 0.000 | 0.025 |
| S | 0.017 | 0.000 | 0.100 |
| Cr | 1.112 | 1.000 | 1.350 |
| Mo | 0.025 | 0.000 | 0.100 |
| Ni | 0.076 | 0.000 | 0.100 |
| Cu | 0.148 | 0.000 | 0.150 |
| N | 0.000 | 0.000 | 0.000 |
| Nb | 0.010 | 0.000 | 0.010 |
| Ti | 0.007 | 0.000 | 0.025 |

Raw Materials

| Name | Qty [t] |
| --- | --- |
| No1 Heavy | 0 |
| No2 Heavy | 0 |
| Internal Low Alloyed | 0 |
| Plate and Structural | 0 |
| eafScrapType05 | 0 |
| No1 Bundles | 23 |
| No2 Bundles | 36 |
| Direct Reduced Iron | 31 |
| Shredded | 0 |
| eafScrapType10 | 0 |
| EAF dust | 0 |
| Turnings | 0 |
| eafAdditive07 | 0 |

Additions

| Name | Qty [t] |
| --- | --- |
| Ferro-Silicon 75, high purity | 0 |
| Ferro-Silicon 75 | 0 |
| Silico-Chromium | 300 |
| Silico-Carbon | 0 |
| Chrome-Carbure | 0 |
| Chrome-Carbure Low S | 2000 |
| Ferro-Molybdenum | 0 |
| Ferro-Vanadium | 0 |
| Aluminum pebbles | 0 |
| Carbon | 200 |
| Iron Oxide | 0 |
| Fluorspar | 0 |
| Dolomite | 2100 |
| Lime | 300 |
| High C Ferro-Manganese | 0 |
| Low C Ferro-Manganese | 0 |

Slag Composition

| Element | Current | Min | Max |
| --- | --- | --- | --- |
| Al2O3 | 4.410 |  |  |
| CaO | 18.705 |  |  |
| Cr2O3 | 16.787 |  |  |
| FeO | 40.957 | 10 | 50 |
| MgO | 8.464 | 8 | 12 |
| MnO | 0.128 |  |  |
| SiO2 | 10.178 |  |  |
| P | 0.344 |  |  |
| S | 0.015 |  |  |
| Basicity | 1.8378054497534 | 1.5 | 2.5 |

Event Log

[
"00:00:00,Selected%20user%20level::%20undefined",
"00:00:00,Selected%20steel%20grade::%20Engineering%20Steel",
"00:00:05,Simulation%20rate%20changed:%2030",
"00:01:23,Scrap%20basket%20added%20with:%20No1%20Bundles:%2023t;%20No2%20Bundles:%2025t",
"00:02:39,Power%20set%20to:%20120%20MW",
"00:03:15,Simulation%20rate%20changed:%201",
"00:04:05,Additions:%20Carbon:%20200%20kg;%20Chrome-Carbure%20Low%20S:%202000%20kg;%20Silico-Chromium:%20300%20kg;%20Dolomite:%202100%20kg;%20Lime:%20300%20kg",
"00:04:07,Simulation%20rate%20changed:%2032",
"00:17:14,Simulation%20rate%20changed:%201",
"00:17:15,Power%20set%20to:%2075%20MW",
"00:17:17,Simulation%20rate%20changed:%2010",
"00:17:24,Simulation%20rate%20changed:%206",
"00:17:59,Simulation%20rate%20changed:%205",
"00:18:20,Simulation%20rate%20changed:%209",
"00:19:12,Simulation%20rate%20changed:%201",
"00:19:14,Oxygen%20flow%20changed%20(150%20Nm%C2%B3%20/%20min)",
"00:19:16,Simulation%20rate%20changed:%2029",
"00:20:03,Power%20set%20to:%200%20MW",
"00:26:40,Simulation%20rate%20changed:%2032",
"00:30:03,Simulation%20rate%20changed:%201",
"00:30:03,Oxygen%20flow%20changed%20(0%20Nm%C2%B3%20/%20min)",
"00:30:06,Simulation%20rate%20changed:%2032",
"00:31:47,Scrap%20basket%20added%20with:%20No2%20Bundles:%2011t;%20Direct%20Reduced%20Iron:%2031t",
"00:32:25,Simulation%20rate%20changed:%201",
"00:32:29,Simulation%20rate%20changed:%209",
"00:33:32,Power%20set%20to:%20120%20MW",
"00:33:49,Simulation%20rate%20changed:%2032",
"00:44:26,Simulation%20rate%20changed:%201",
"00:44:27,Power%20set%20to:%2075%20MW",
"00:44:29,Simulation%20rate%20changed:%207",
"00:45:07,Simulation%20rate%20changed:%2010",
"00:46:22,Oxygen%20flow%20changed%20(150%20Nm%C2%B3%20/%20min)",
"00:46:37,Simulation%20rate%20changed:%2030",
"00:49:52,Power%20set%20to:%200%20MW",
"01:08:56,Analysis%20Requested",
"01:11:17,Simulation%20rate%20changed:%201",
"01:11:18,Simulation%20rate%20changed:%206",
"01:11:24,Simulation%20rate%20changed:%201",
"01:11:24,Simulation%20rate%20changed:%206",
"01:11:31,Simulation%20rate%20changed:%201",
"01:11:31,Simulation%20rate%20changed:%207",
"01:11:37,Simulation%20rate%20changed:%201",
"01:11:37,Simulation%20rate%20changed:%208",
"01:11:44,Simulation%20rate%20changed:%201",
"01:11:44,Simulation%20rate%20changed:%206",
"01:11:47,Simulation%20rate%20changed:%207",
"01:11:49,Simulation%20rate%20changed:%208",
"01:11:53,Simulation%20rate%20changed:%201",
"01:11:54,Simulation%20rate%20changed:%204",
"01:11:56,Analysis%20received",
"01:11:57,Simulation%20rate%20changed:%201",
"01:11:59,Oxygen%20flow%20changed%20(0%20Nm%C2%B3%20/%20min)",
"01:12:01,Simulation%20rate%20changed:%2032",
"01:13:56,Tapping%20start",
"01:15:46,Tapping%20complete"
]