Electric Arc Furnace

Comments

Run Information

| User Id | taehee0518@daum.net |
| --- | --- |
| Date | 13/07/2024 10:07:35 |
| Status | 0 |
| Score | $ 454.53 |

Simulation settings

| User Level | University Student |
| --- | --- |
| Steel Grade | Engineering Steel |

Cost Breakdown

| Time (in minutes) | 79 |
| --- | --- |
| Tapping mass | 87 |
| Tap temperature | 1634 |
| Total Energy | 35614 kWh |
| Total Energy | 408 kWh/t |
| Power | $ 1736 |
| Scrap | $ 79 |
| Additions | $ 17080 |
| Other consumables | $ 20299.97 |
| Total Cost | $ 39632 |
| Cost Per Tonne | $ 454.53 |

Steel Composition / wt%

| Element | Current | Min | Max |
| --- | --- | --- | --- |
| C | 1.089 | 1.050 | 1.150 |
| Si | 0.127 | 0.100 | 0.150 |
| Mn | 0.220 | 0.150 | 0.250 |
| P | 0.011 | 0.000 | 0.025 |
| S | 0.017 | 0.000 | 0.100 |
| Cr | 1.110 | 1.000 | 1.350 |
| Mo | 0.024 | 0.000 | 0.100 |
| Ni | 0.075 | 0.000 | 0.100 |
| Cu | 0.146 | 0.000 | 0.150 |
| N | 0.000 | 0.000 | 0.000 |
| Nb | 0.010 | 0.000 | 0.010 |
| Ti | 0.007 | 0.000 | 0.025 |

Raw Materials

| Name | Qty [t] |
| --- | --- |
| No1 Heavy | 0 |
| No2 Heavy | 0 |
| Internal Low Alloyed | 0 |
| Plate and Structural | 0 |
| eafScrapType05 | 0 |
| No1 Bundles | 23 |
| No2 Bundles | 36 |
| Direct Reduced Iron | 31 |
| Shredded | 0 |
| eafScrapType10 | 0 |
| EAF dust | 0 |
| Turnings | 0 |
| eafAdditive07 | 0 |

Additions

| Name | Qty [t] |
| --- | --- |
| Ferro-Silicon 75, high purity | 0 |
| Ferro-Silicon 75 | 0 |
| Silico-Chromium | 300 |
| Silico-Carbon | 0 |
| Chrome-Carbure | 0 |
| Chrome-Carbure Low S | 1700 |
| Ferro-Molybdenum | 0 |
| Ferro-Vanadium | 0 |
| Aluminum pebbles | 0 |
| Carbon | 200 |
| Iron Oxide | 0 |
| Fluorspar | 0 |
| Dolomite | 2100 |
| Lime | 200 |
| High C Ferro-Manganese | 0 |
| Low C Ferro-Manganese | 0 |

Slag Composition

| Element | Current | Min | Max |
| --- | --- | --- | --- |
| Al2O3 | 5.326 |  |  |
| CaO | 21.664 |  |  |
| Cr2O3 | 13.201 |  |  |
| FeO | 37.219 | 10 | 50 |
| MgO | 10.178 | 8 | 12 |
| MnO | 0.156 |  |  |
| SiO2 | 11.846 |  |  |
| P | 0.383 |  |  |
| S | 0.015 |  |  |
| Basicity | 1.82886327436642 | 1.5 | 2.5 |

Event Log

[
"00:00:00,Selected%20user%20level::%20undefined",
"00:00:00,Selected%20steel%20grade::%20Engineering%20Steel",
"00:00:07,Simulation%20rate%20changed:%2018",
"00:01:18,Scrap%20basket%20added%20with:%20No1%20Bundles:%2023t;%20No2%20Bundles:%2025t",
"00:02:18,Power%20set%20to:%20120%20MW",
"00:02:50,Simulation%20rate%20changed:%201",
"00:03:32,Additions:%20Carbon:%20200%20kg;%20Chrome-Carbure%20Low%20S:%201500%20kg;%20Silico-Chromium:%20300%20kg;%20Dolomite:%202100%20kg;%20Lime:%20200%20kg",
"00:03:34,Simulation%20rate%20changed:%2032",
"00:17:25,Simulation%20rate%20changed:%202",
"00:17:27,Power%20set%20to:%2075%20MW",
"00:17:39,Simulation%20rate%20changed:%206",
"00:17:55,Simulation%20rate%20changed:%201",
"00:17:59,Oxygen%20flow%20changed%20(100%20Nm%C2%B3%20/%20min)",
"00:18:01,Simulation%20rate%20changed:%207",
"00:18:11,Oxygen%20flow%20changed%20(0%20Nm%C2%B3%20/%20min)",
"00:18:15,Oxygen%20flow%20changed%20(100%20Nm%C2%B3%20/%20min)",
"00:18:38,Simulation%20rate%20changed:%2017",
"00:19:35,Power%20set%20to:%200%20MW",
"00:19:59,Simulation%20rate%20changed:%2032",
"00:30:38,Oxygen%20flow%20changed%20(0%20Nm%C2%B3%20/%20min)",
"00:33:10,Scrap%20basket%20added%20with:%20No2%20Bundles:%2011t;%20Direct%20Reduced%20Iron:%2031t",
"00:35:42,Power%20set%20to:%2075%20MW",
"00:36:48,Power%20set%20to:%20105%20MW",
"00:48:34,Power%20set%20to:%2075%20MW",
"00:49:41,Simulation%20rate%20changed:%203",
"00:49:45,Simulation%20rate%20changed:%2011",
"00:50:28,Oxygen%20flow%20changed%20(100%20Nm%C2%B3%20/%20min)",
"00:50:40,Simulation%20rate%20changed:%2031",
"00:54:57,Power%20set%20to:%200%20MW",
"00:58:31,Simulation%20rate%20changed:%208",
"01:00:24,Analysis%20Requested",
"01:00:40,Oxygen%20flow%20changed%20(110%20Nm%C2%B3%20/%20min)",
"01:00:40,Oxygen%20flow%20changed%20(120%20Nm%C2%B3%20/%20min)",
"01:00:40,Oxygen%20flow%20changed%20(130%20Nm%C2%B3%20/%20min)",
"01:00:41,Oxygen%20flow%20changed%20(140%20Nm%C2%B3%20/%20min)",
"01:00:43,Oxygen%20flow%20changed%20(150%20Nm%C2%B3%20/%20min)",
"01:00:54,Simulation%20rate%20changed:%2032",
"01:03:23,Simulation%20rate%20changed:%201",
"01:03:23,Simulation%20rate%20changed:%205",
"01:03:27,Analysis%20received",
"01:05:03,Simulation%20rate%20changed:%2023",
"01:07:09,Simulation%20rate%20changed:%201",
"01:07:23,Analysis%20Requested",
"01:07:24,Simulation%20rate%20changed:%2032",
"01:10:12,Simulation%20rate%20changed:%201",
"01:10:22,Simulation%20rate%20changed:%206",
"01:10:23,Analysis%20received",
"01:12:28,Additions:%20Chrome-Carbure%20Low%20S:%20200%20kg",
"01:12:53,Simulation%20rate%20changed:%2013",
"01:14:00,Power%20set%20to:%2075%20MW",
"01:14:32,Power%20set%20to:%200%20MW",
"01:17:12,Oxygen%20flow%20changed%20(0%20Nm%C2%B3%20/%20min)",
"01:17:54,Tapping%20start",
"01:19:44,Tapping%20complete"
]