Electric Arc Furnace

Comments

Run Information

| User Id | taehee0518@daum.net |
| --- | --- |
| Date | 13/07/2024 11:07:05 |
| Status | 0 |
| Score | $ 442.98 |

Simulation settings

| User Level | University Student |
| --- | --- |
| Steel Grade | Engineering Steel |

Cost Breakdown

| Time (in minutes) | 62 |
| --- | --- |
| Tapping mass | 87 |
| Tap temperature | 1638 |
| Total Energy | 34675 kWh |
| Total Energy | 398 kWh/t |
| Power | $ 1420.4 |
| Scrap | $ 62 |
| Additions | $ 17080 |
| Other consumables | $ 19765.00 |
| Total Cost | $ 38639 |
| Cost Per Tonne | $ 442.98 |

Steel Composition / wt%

| Element | Current | Min | Max |
| --- | --- | --- | --- |
| C | 1.069 | 1.050 | 1.150 |
| Si | 0.107 | 0.100 | 0.150 |
| Mn | 0.220 | 0.150 | 0.250 |
| P | 0.021 | 0.000 | 0.025 |
| S | 0.015 | 0.000 | 0.100 |
| Cr | 1.154 | 1.000 | 1.350 |
| Mo | 0.024 | 0.000 | 0.100 |
| Ni | 0.075 | 0.000 | 0.100 |
| Cu | 0.147 | 0.000 | 0.150 |
| N | 0.000 | 0.000 | 0.000 |
| Nb | 0.010 | 0.000 | 0.010 |
| Ti | 0.007 | 0.000 | 0.025 |

Raw Materials

| Name | Qty [t] |
| --- | --- |
| No1 Heavy | 0 |
| No2 Heavy | 0 |
| Internal Low Alloyed | 0 |
| Plate and Structural | 0 |
| eafScrapType05 | 0 |
| No1 Bundles | 23 |
| No2 Bundles | 36 |
| Direct Reduced Iron | 31 |
| Shredded | 0 |
| eafScrapType10 | 0 |
| EAF dust | 0 |
| Turnings | 0 |
| eafAdditive07 | 0 |

Additions

| Name | Qty [t] |
| --- | --- |
| Ferro-Silicon 75, high purity | 0 |
| Ferro-Silicon 75 | 0 |
| Silico-Chromium | 200 |
| Silico-Carbon | 0 |
| Chrome-Carbure | 0 |
| Chrome-Carbure Low S | 1500 |
| Ferro-Molybdenum | 0 |
| Ferro-Vanadium | 0 |
| Aluminum pebbles | 0 |
| Carbon | 180 |
| Iron Oxide | 0 |
| Fluorspar | 0 |
| Dolomite | 1500 |
| Lime | 100 |
| High C Ferro-Manganese | 0 |
| Low C Ferro-Manganese | 0 |

Slag Composition

| Element | Current | Min | Max |
| --- | --- | --- | --- |
| Al2O3 | 6.484 |  |  |
| CaO | 19.690 |  |  |
| Cr2O3 | 7.317 |  |  |
| FeO | 43.040 | 10 | 50 |
| MgO | 9.018 | 8 | 12 |
| MnO | 0.189 |  |  |
| SiO2 | 13.892 |  |  |
| P | 0.329 |  |  |
| S | 0.026 |  |  |
| Basicity | 1.41731462566256 | 1.5 | 2.5 |

Event Log

[
"00:00:00,Selected%20user%20level::%20undefined",
"00:00:00,Selected%20steel%20grade::%20Engineering%20Steel",
"00:00:05,Simulation%20rate%20changed:%2032",
"00:01:45,Scrap%20basket%20added%20with:%20No1%20Bundles:%2023t;%20No2%20Bundles:%2025t",
"00:03:17,Power%20set%20to:%20120%20MW",
"00:04:00,Simulation%20rate%20changed:%201",
"00:04:11,Additions:%20Dolomite:%201500%20kg;%20Lime:%20100%20kg",
"00:04:13,Simulation%20rate%20changed:%2032",
"00:13:37,Simulation%20rate%20changed:%201",
"00:14:00,Simulation%20rate%20changed:%2019",
"00:14:35,Simulation%20rate%20changed:%2032",
"00:18:01,Simulation%20rate%20changed:%201",
"00:18:02,Power%20set%20to:%2075%20MW",
"00:18:07,Simulation%20rate%20changed:%2010",
"00:18:21,Oxygen%20flow%20changed%20(150%20Nm%C2%B3%20/%20min)",
"00:19:30,Power%20set%20to:%200%20MW",
"00:20:41,Simulation%20rate%20changed:%2032",
"00:30:21,Oxygen%20flow%20changed%20(0%20Nm%C2%B3%20/%20min)",
"00:32:44,Scrap%20basket%20added%20with:%20No2%20Bundles:%2011t;%20Direct%20Reduced%20Iron:%2031t",
"00:34:38,Power%20set%20to:%2075%20MW",
"00:35:11,Power%20set%20to:%20120%20MW",
"00:45:08,Simulation%20rate%20changed:%202",
"00:45:11,Simulation%20rate%20changed:%2012",
"00:45:34,Power%20set%20to:%2075%20MW",
"00:46:22,Simulation%20rate%20changed:%201",
"00:46:26,Simulation%20rate%20changed:%207",
"00:47:31,Simulation%20rate%20changed:%201",
"00:47:42,Simulation%20rate%20changed:%208",
"00:48:30,Oxygen%20flow%20changed%20(150%20Nm%C2%B3%20/%20min)",
"00:48:52,Simulation%20rate%20changed:%201",
"00:49:31,Additions:%20Carbon:%20150%20kg;%20Chrome-Carbure%20Low%20S:%201200%20kg;%20Silico-Chromium:%20200%20kg",
"00:49:34,Simulation%20rate%20changed:%208",
"00:50:08,Simulation%20rate%20changed:%2014",
"00:50:18,Simulation%20rate%20changed:%201",
"00:50:20,Simulation%20rate%20changed:%2017",
"00:52:13,Power%20set%20to:%200%20MW",
"00:53:57,Power%20set%20to:%2075%20MW",
"00:54:29,Power%20set%20to:%200%20MW",
"00:54:44,Analysis%20Requested",
"00:55:02,Simulation%20rate%20changed:%2032",
"00:56:23,Simulation%20rate%20changed:%201",
"00:56:24,Simulation%20rate%20changed:%2032",
"00:57:44,Analysis%20received",
"00:58:05,Simulation%20rate%20changed:%201",
"00:58:30,Additions:%20Chrome-Carbure%20Low%20S:%20300%20kg",
"00:58:31,Power%20set%20to:%2075%20MW",
"00:58:37,Simulation%20rate%20changed:%206",
"00:58:42,Simulation%20rate%20changed:%201",
"00:58:43,Power%20set%20to:%200%20MW",
"00:58:48,Simulation%20rate%20changed:%2010",
"00:58:56,Simulation%20rate%20changed:%201",
"00:59:10,Additions:%20Carbon:%2030%20kg",
"00:59:11,Power%20set%20to:%2075%20MW",
"00:59:13,Power%20set%20to:%200%20MW",
"00:59:17,Power%20set%20to:%2075%20MW",
"00:59:19,Simulation%20rate%20changed:%209",
"00:59:34,Power%20set%20to:%200%20MW",
"00:59:39,Oxygen%20flow%20changed%20(0%20Nm%C2%B3%20/%20min)",
"01:01:06,Tapping%20start",
"01:02:57,Tapping%20complete"
]